Mechanistic Insights into the Deoxygenation of Biomass-derived 6-amyl-α-pyrone: Experimental and DFT Insights

Aishwarya Narayanan1, *Shelaka Gupta1

1 Chemical Engineeirng, Indian Institiute of Technology Hyderabad, India

*Corresponding Author's E-mail address: shelaka@che.iith.ac.in

Abstract Category: Environmentaly-friendly and Sustainable Chemicals - Sustainable Chemicals - Biomass

Keywords: Hydrodeoxygenation, Ir-ReOx/SiO2 catalyst, 6-amyl-α-pyrone

Abstract Body.

Advances in metabolic engineering have enabled the production of various platform molecules with varying carbon chain lengths directly from the fermentation of biomass-derived aqueous sugars. Catalytic conversion of these has received attention to producing value-added chemicals like n-alkanes [1], which were principally derived from crude oil. Therefore, a novel strategy is proposed in which 6-amyl-α-pyrone (6-PP), obtained from solid-state fermentation of biomass, is directly converted to n-decane, a fuel additive, in a single step using a bifunctional catalyst without the loss of any carbon atoms.Ir-ReOx/SiO2catalyst (Re/Ir = 0.5) exhibited maximum conversion of 6-PP (99.8%) and n-decane selectivity of 81.8% at 473 K and 7 MPa in 14 hours. DFT simulations showed that on Ir (111) surface, the activation barrier for C2-O1 cleavage of 6-PP was 79.9 kJ/mol, which reduced to 50.9 kJ/mol on the Re3O6H2/Ir interface (Figure 1, (i)), explaining the relevance of Ir-ReOxinterphase in enabling efficient C-O bond cleavage. Further, to reduce the cost of the catalyst, ReOxwas replaced with cheaper promoters like WOx, VOx, NbOxand MoOxin which Ir-MoOx/SiO2(Mo/Ir=0.25) catalyst exhibited maximum n-decane selectivity of 88.1 % and conversion of 96.4 %. Overall, this integration pathway enabled the production of long-chain alkane (n-decane) from 6-PP however, the presence of biogenic impurities in the fermentation broth along with 6-PP may lead to catalyst deactivation. Therefore, HDO of 6-PP on Ir-ReOx/SiO2catalyst was carried in presence of impurities like Alanine, Arginine, Methionine, and Cysteine. Interestingly, 100 ppm of sulfur-containing impurities cysteine and methionine caused a significant decrease in 6-PP conversion (Table1, entries 4 & 5). This decrease in 6-PP conversion can be attributed to much stronger adsorption of impurities on the catalyst surface(Figure 1, (ii)). Alanine showed no effect, whereas Arginine was observed to cause only a moderate reduction in conversion (Table1, entries 2&3). Together, these studies establish how rational catalyst design critically governs deoxygenation pathways, providing valuable guidance for biomass valorization.

References

1.Alam, M. Iet al.Green Chemistry,2016, 8, 24, 6431-6435.

2.Yoshinao Nakagawaet al,Journal of Catalysis2010, 272, 191-194